PROFLOOR X

825

MMA Resin Based General Purpose Floor Paint

PRODUCT DESCRIPTION:

MMA based, solvent based, glossy appearance, floor paint.

FEATURES:

It has high covering power. It is resistant to rain and

water. Quick and easy to apply. High mechanical strength. Does

not fade or yellow over time. Resistant to abrasion. It is not

affected by human and vehicle traffic. Can be used on vertical

and horizontal surfaces. Covers the surface perfectly

homogeneous. Quickly applied. Prevents dusting. Bright

appearance.

PRODUCT INFORMATION:

Chemical Structure 			Acrylic based / Solvent based

View / Color 				Liquid / Contact

Density 				1.30 ± 0.2 g / cm3

# PERFORMANCE:

(23°C, %50 Relative Humidity)

Density		1,30 ±0,2 g / cm3

These values are obtained as a result of laboratory tests and are valid for the performance of finished applications at the end of full drying time. Since the temperature and humidity values in the construction site and the application surface vary, given values might be diversing.

APPLICATION AREA:

Concrete, screed and paving stones,

Internal and external applications,

Warehouses and factories,

Shopping centers, supermarkets,

For warehouse floors,

Tourist facilities, bike paths, coastline, walking paths, squares, parks and gardens.

PROFLOOR X

825

MMA Resin Based General Purpose Floor Paint

APPLICATION INSTRUCTIONS:

The surface should be cured, dry and sound. Remove any oil, grease, dirt, dust, etc. that will

prevent adhesion. Ready to use. Then It should be mixed product until it containes a homogenous consistency by up to 400 rpm mixer.. Directly applied. Product can be applied

with roller or spraying equipment. To achieve optimum quality, please follow the instructions for use. It should not be applied in very windy, rainy weather which is directly

exposed to sunlight at very high temperature. Application should not be applied on surfaces with frost hazard. Application should be between +5 C and +30 C. Do not apply at temperatures below 5 ° C. 24 hours after the application, rain, water, frost and adverse effects should be protected from external factors.

Application Equipment:

Hand Mixer

Roll

# LIMITATIONS:

To achieve optimum quality, please follow the instructions for use. It should not be applied in very windy, rainy weather which is directly exposed to sunlight at very high temperature. Application should not be applied on surfaces with frost hazard. Application should be between +5 C and +30 C. Do not apply at temperatures below 5 ° C. 24 hours after the application, rain, water, frost and adverse effects should be protected from external factors.

CONSUMPTION:

300-500 gr/m2

PACKING:

18kg tin packaging

PROFLOOR X

825

MMA Resin Based General Purpose Floor Paint

SHELF LIFE:

It is 1 year from the date of production in its original packaging in dry and dry (+5 C to +25 C) environments. The mouth of the containers should be tightly closed when not in use. It should be kept away from moisture.

STORAGE CONDITIONS:

It should be stored in its original unopened package in a cool, dry and humid-free (+5 C to +25 C temperature) environment. Should not be left in direct sunlight.

# SAFETY:

Avoid contact with skin and eyes. Wear protective gloves, glasses, mask and clothing. In case of eye contact, consult a doctor immediately. Keep out of the reach of children. Avoid skin contact. Do not swallow. Keep away from sources of ignition. For further information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product.