PROLASTIC

MEGA

230

Cement Acrylic Based Double Component Super Elastic Water Insulation Product

# PRODUCT DESCRIPTION:

It is a two-component, cement-based, polymer-emulsion, special chemicals containing gray colored full elastic waterproofing mortar resistant to light pedestrian traffic.

FEATURES :

It has high elasticity. Crack bridging feature is high. Adherence is strong. Excellent adhesion to mineral surfaces. Resistant to frost thaw cycle.

PRODUCT INFORMATION:

Powder Component:

Chemical Structure Cement based

Appearance / Color Powder / Gray

Liquid Component:

Chemical Structure       Acrylic-based / Water-based

Appearance /               Color Liquid / White

Dry Film                       Color Transparent

Ph5-7

# PERFORMANCE:

(23°C, %50 RH )

Dry Bulk Density (powder component)	1650 ± 200 kg/m3	TS EN 1015-10

Density (liquid component)		0,98-1,1 gr/cm3

Crack bridging			≥ 1,2 mm		TS EN 1062-7 (+23 °C)

Capillary water absorption		<0,1 kg/m2.h0,5	TS EN 1062-3

Adhesion to Concrete			≥ 0,5 MPa		TS EN 1542

These values were obtained as a result of laboratory experiments and are valid for the performance of finished applications at the end of the complete drying period. The values may change as the temperature and humidity values in the workplace environment and the application surfaces and areas will vary.

# APPLICATION AREAS :

It is applied under the tiles on the mineralsurfaces such as concrete, plaster, screed, on balconies and terraces, in wet areas such as bathrooms, toilets and kitchens.

Used for waterproofing from passive side, remaning structuresabove the soil.

PROLASTIC

MEGA

230

Cement Acrylic Based Double Component Super Elastic Water Insulation Product

# APPLICATION INSTRUCTION:

The application surfaces should be moist and dry surfaces should be moistened before

application. The surface must be cured and intact. It should be cleaned from residues such as oil, grease, dirt, paint and salt vomiting which will prevent adhesion. If

there is a surface defect, it should be repaired with PROREPAIR THIN or PROREPAIR at least 24 hours in advance. It is recommended to apply PROGEN PR before

application on highly porous surfaces. It prevents salt vomiting. Corners and joints must be turned with PROBAND waterproofing chamfering tape. Slowly pour

20 kg powder component into 10 kg. liquid component and mix with low speed mixer until there is no lump. Do not add water. Allow the mortar to mature for 3-5 minutes.

Mix again before application. Apply with brush, trowel or suitable spraying equipment. It should be applied as 2 -3 layers on the surface. The application of each layer should

be caged in a direction perpendicular to the previous one. Wait at least 12 hours between coats. Total layer thickness should be 2-3 mm. It is recommended that the process be completed within a maximum of 2-3 hours in order to make the most of the product. Protective layer such as screed and ceramic should be applied on places with traffic load and in open areas. Expired mortar should be disposed of.

Application Equipment:

Hand mixer

Trowel

Brush & Roll

# LIMITATION:

# In order to obtain optimum quality, please stick to the application instructions. Application should be done between +5 C and +30 C. It should not be applied in very windy and rainy weather conditions exposed to sunlight directly at very high temperatures. It should not be applied on the surfaces with the risk of frost. The product should be protected from rain, water, frost and adverse external factors until it is cured (28 days)..

# CONSUMPTION:

3-3.5 kg / m2 for 2 mm thickness.

PROLASTIC

MEGA

230

Cement Acrylic Based Double Component Super Elastic Water Insulation Product

# PACKING :

Powder component: in 20 kg craft bag

Liquid component: 10 lt bag can

# SHELF LIFE:

It is 1 year from the date of production in its original packaging in humid-free  and dry (+5 C to +25 C) environments. The products should be tightly closed when not in use. It should be kept away from moisture.

STORAGE CONDITIONS:

It should be stored in its original unopened package, in a dry, humid-free and cool place (temperature between +5 C and +25 C). It should not be left under direct sunlight.

# SAFETY:

Considering it is a cement based, do not breathe the dust, use a mask. Avoid contact with skin and eyes. Use protective gloves, goggles and clothing. In case of eye contact, wash with plenty of water and consult a doctor immediately. Keep out of the reach of children. In case of skin contact, wash with plenty of soap and water. Do not swallow. For detailed information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product