PROPOLBITUM

360

Bitumen - Polyurethane Based Double Component Waterproofİng Product

PRODUCT DESCRIPTION:

It is a two component, polyurethane based and fast curing, elastic, cold applied liquid membrane containing bitumen. It forms a film with high elasticity by adhering perfectly to almost any surface it is applied to.

It cures chemically to form an elastic and durable film.

FEATURES:

Easy to apply (with brush, roller or airless spray).

When applied, it forms a one-piece waterproofing layer, which does not require joint formation or leakage.

Flexibility is quite high.

Fast curing.

Excellent mechanical properties, elongation, tensile, tear and abrasion resistance is high.

It is resistant to stagnant water and frost.

The heat resistance performance over a wide temperature range is between -40 ° C and + 90 ° C.

Even if the waterproofing layer is damaged in any way, the damaged part can be easily repaired in a short time.

It can also be used as a joint material.

Resistant to chemicals.

PRODUCT INFORMATION:

Chemical Structure 		Polyurethane-Bitumen

Appearance / Color 		Liquid / Black

PERFORMANCE:

(23 ° C, 50% RH)

Density			: 1.0 gr / cm3 ± 0.02 	ASTM D 1475 / EN ISO 2811-1 (20 ° C)

Viscosity			: 3000-3500 cp 	ASTM D 2196 / EN ISO 3219 (25 ° C)

Hardness			: 70 (Shore A) 	ASTM 02240

Adhesion to concrete		:> 2 N / mm2 		ASTM D 903

Breakdown			:> 2 N / mm2

Water Vapor Permeability	: 0.8 gr / m² per hour

QUV				: 2000 HOURS 	ASTM D 412

Elasticity			: > 2000%

Drying time			: 2 hours

Re-laying			: 12-24 hours

Full Drying			: 7 days

These values are obtained as a result of laboratory tests and are valid for the performance of finished applications at the end of full drying time. Since the temperature and humidity values in the construction site and the application surface vary, given values might be diversing.

PROPOLBITUM

360

Bitumen - Polyurethane Based Double Component Waterproofİng Product

APPLICATION AREAS:

Water tanks (excluding drinking water tanks),

Floors,

Foundations,

Bridge platforms,

Open-close tunnels,

It is applied under the tiles in bathrooms, terraces and roofs.

Concrete structures,

Retaining walls,

Gypsum and cement panels,

EPDM membranes,

Asphalt membranes.

Green roofs and plant beds,

Light roofs (made of metal or fibrous cement)

Parking Lots

APPLICATION INSTRUCTIONS:

The surface should be cured, dry and sound. Remove oil, grease, dirt, paint and salt vapors that would prevent adhesion. If the surface is cracked or broken, it should be repaired at least 24h beforehand with PROREPAIR PLUS, PROMORTAR EPO or PROEPO ANCHOR. Corrections should be corrected that may cause ponding. The application surface should be smooth, bowless.

A component and component B must be mixed with a medium speed mixer at 400-600 rpm until a homogeneous mixture is obtained. Do not add or dilute any substances.

Application Equipments:

Roller brush

Surface should be primed with PROPOL PR, PROPOL PR WT or suitable primer. By Brush, trowel, spatula should be applied to prepared surface. Prepared mixture should be consumed in 30 min. The mixture starting to gel must not be used. By pouring on the primed surface or by dipping into bucket, min. should be applied in two layers. After applying the first layer, in min. 12, max. 24 hours, second layer should be applied. Waiting times between layers should not exceed 48 hours. After application, the tools should be cleaned within 2 hours.

PROPOLBITUM

360

Bitumen - Polyurethane Based Double Component Waterproofİng Product

# LIMITATIONS:

To achieve optimum quality, please follow the instructions for use. Application should be made to the part of the structure in contact with water. Since the curing of the material will be slower in cold weather, it should be ensured that the first layer is completely dry without applying the 2nd layer. It should not be applied in very windy, rainy weather, enviorenments which is directly exposed to sunlight, and very high temperature. The first 24 hours after application should be protected from frost, sun and strong wind. Application should not be applied on surfaces with frost hazard. Application should be between +5 C and +30 C. Do not apply at temperatures below 5 ° C.

CONSUMPTION:

For each layer					0,750 - 1,00 Kg / m²

Total theoretical consumption (2 layers)	1,50 - 2,00 Kg / m²

PACKING:

A: 20KG B: 20KG tin packaging

A: 7.5KG B: 7.5KG tin packaging

# SHELF LIFE:

In its original package with closed lid, Its 1 year from the date of production in dry and humid-free, no direct sunlight recieving spaces in between ,+5 ̊ - 25   ̊C under the %50 relative humidty. When not in use, cover packaging tightly. Keep away from moisture. Protect from high temperatures and frost.

STORAGE CONDITIONS:

In its original package, it should be stored in a cool, dry (+5 C to +25 C temperature) environment. It should not be left under direct sunlight.

SAFETY:

Do not breathe, wear a mask. Avoid contact with skin and eyes. Wear protective gloves, glasses and clothing. In case of eye contact, consult a doctor immediately. Keep out of the reach of children. In case of contact with skin, wash with plenty of water and soap. Do not swallow. For further information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product