PROLEVEL

515

Cement Based Self-Levelling Screed

# PRODUCT DESCRIPTION:

# It is a cement based, self-leveling screed containing hyper plasticizers that can be applied between 1-10 mm in a single layer and can provide easy application.

FEATURES :

Suitable for floors exposed to moderate and heavy pedestrian traffic.

Spreads automatically to the balance.

Suitable for application of 1-10 mm thickness without shrinkage crack formation.

Resistant to abrasion. It has high adherence due to its special polymer.

PRODUCT INFORMATION:

Chemical Structure	Cement Based

Appereance /Color	Powder/Grey

# PERFORMANCE:

# (23°C, %50 Relative Humidity)

# Dry Bulk Density		1350 ± 200 kg/m3	TS EN 1015-10

# Capillary Water Absorption	≤ 0,5 gr 		TS EN 1015-18

These values were obtained as a result of laboratory experiments carried out in our company and are valid for the performance of finished applications at the end of the complete drying period. The values may change as the temperature and humidity values in the workplace environment and application surfaces will vary.

PROLEVEL

515

# Cement Based Self-Levelling Screed

# APPLICATION AREAS:

# It is used to create a solid and smooth floor against abrasion and dusting on the surfaces exposed to medium and heavy traffic of all buildings before final coating. It can be use on PVC, laminate flooring, wood, carpet, under the ceramic coating, after floor insulation, cement-based surfaces to smooth.

# APPLICATION INSTRUCTIONS:

# The surface must be cured, dry and intact. Oil, grease, dirt, paint, salt and vomiting should be

# removed from the surface to prevent adhesion. The surface should be roughened. Cracked and hollow areas on the surface should be repaired by PROREPAIR THIN or PROREPAIR;

# PROREPAIR PLUS should be used to repair at least 24 hours in advance if the application will be made in environments exposed to high sulphate such as sea water, sewage. Slowly pour 25 kg of PROLEVEL onto 6 -7 lt water and mix with low speed mixer until there is no lump. Allow the mortar to mature for 3-5 minutes. Mix again before application.

Application Equipments:

Hand Mixer

Steel Trowel

# Hedgehog roll

# The prepared mortar is poured onto the surface starting from a corner and spreading by itself. The thickness of the selfleveling mortar should be adjusted with a steel trowel. Smooth

# the surface with a spiked roller to prevent air bubbles. If coating is to be applied, it can be done after 24 hours. It is recommended that the process be completed within a maximum of 15-20 minutes for maximum utilization of the product due to its expansion properties. Expired mortar should be disposed of.

# LIMITATIONS:

# To achieve optimum quality, please stick to the application instructions. Application should be done between +5 C and +30 C. Application should not be done in hot, rainy and windy weather. It should not be applied on the surfaces with the risk of frost. The product should be protected from rain, water, frost and adverse external factors until it cures (28 days).

# CONSUMPTION:

# 1,3-1,5 kg/m2 (For 1 mm. Thickness layer) 10 mm. Max application thickness.

PROLEVEL

515

Cement Based Self-Levelling Screed

# PACKING:

# 25 kg Craft Bag

# (palette 64 pcs, 1600 kg)

# COLOR:

# Grey.

# SHELF LIFE:

In humid-free and dry (+5 C to +25 C temperature) space in the original package 1 year from the date of production. The lid of the containers should be tightly closed when not in use. Keep away from moisture

STORAGE CONDITIONS:

It should be stored in its original unopened package in a humid-free, dry and cool (+5 C to +25 C temperature) environment. Should not be exposed to direct sunlight.

SAFETY:

Considering it is a cement based, do not breathe dust, use a mask. Avoid contact with skin and eyes. Wear protective gloves, goggles and clothing. In case of eye contact rinse with plenty of water and seek medical advice immediately. Keep out of the reach of children. In case of contact with skin, wash with plenty of water and soap. Do not swallow. For further information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR. DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product