PROMARBLE MAX 495

Cement Based High Performance Flexible Granıte And Marble White Adhesive Mortar

C2TES1

PRODUCT DESCRIPTION:

It is cement based, high performance, flexible,reduced slip, deformable, white

colored granite and marble bonding mortar.

FEATURES :

High performance. Water, moisture and impact

resistant. The convenience of setting time provides ease of

application and does not require much labor. High adhesion

strength. High adherence. Suitable for ceramic flooring from top

to bottom and horizontally. Easy to comb.

PRODUCT INFORMATION:

# Chemical Structure                   Cement based

# Appearance /                            Color Powder / White

# Pot Life                                     1 hour

# C                                               Cement based

# 2                                                High Performance Adhesives

# T                                                Slip feature reduced

# E                                                Extended Open Time

S1 Shape may be distorted

# PERFORMANCE

(23°C, %50 RH )

Tensile Adhesion			≥ 0,5 N/mm2	TS EN 1348

Tensile Adhesion After Water	≥ 0,5 N/mm2	TS EN 1348

Tensile Adhesion After Heat  	≥ 0,5 N/mm2	TS EN 1348

Tensile Adhesion After Freezing	≥ 0,5 N/mm2	TS EN 1348

Open Time After 30 minutes  	≥ 0,5 N/mm2	TS EN 1346

Slip Determination			<0,5 mm

These values were obtained as a result of laboratory experiments carried out in our company and are valid for the performance of finished applications at the end of the complete drying period. The values may change as the temperature and humidity values in the workplace environment and the application surfaces and areas will vary.

# APPLICATION AREAS

In bonding ceramic, tile, marble, granite, natural granite, mosaic, decorative brick, natural stone, etc. coating materials; It can be applied on wet surfaces such as bathrooms, kitchens, surfaces such as concrete, brick and plaster. The surface must be roughened with PROJEL PR before the existing ceramic bonding applications.

PROMARBLE MAX 495

Cement Based High Performance Flexible Granıte And Marble White Adhesive Mortar

C2TES1

# APPLICATION INSTRUCTIONS:

The surface must be cured, dry and intact. It should be cleaned from residues such as oil, grease, dirt, paint and salt vomiting which will prevent adhesion. The surface should be rough. If there are significant defects on the surface to be treated, PROREPAIR THIN or PROREPAIR; PROREPAIR PLUS should be used to repair at least 24 hours in advance if the application will be made in environments exposed to high sulphate such as sea water, sewage. Pour 25 kg of PROMARBLE MAX W slowly into 6-7 liters of water and mix with a low speed mixer until no lumps remain. Allow the mortar to mature for 5-10 minutes. Mix again before application. PROMARBLE MAX W is spread on the surface with a trowel. It is scanned by moving the gear circularly with a trowel. The ceramics are pressed onto the combed mortar and adhered. Joints can be used between the ceramics in order to take the joint filler evenly. The expired or crusted mortar should be disposed of. Surfaces should be cleaned with a damp cloth. Avoid contacting the tiles with water for at least 24 hours.

Application Equipment:

Hand mixer

Trowel

Plastic hammer

Toothed trowel

LIMITATIONS:

In order to obtain optimum quality, please stick to the application instructions. Application should be done between +5 C and +30 C. Application should not be done in hot, rainy and windy weather. It should not be applied on the surfaces with the risk of frost. The product should be protected from rain, water, frost and adverse external factors until it cures (28 days).

CONSUMPTION

3-5 kg/m2.

PACKING:

In 25 kg craft bag,

(64 pieces in pallet, 1600 kg)

PROMARBLE MAX 495

Cement Based High Performance Flexible Granıte And Marble White Adhesive Mortar

C2TES1

SHELF LIFE:

It is 1 year from the date of production in its original packaging in a humid-free , dry and cool (+5 C to +25 C) environment. The mouth of the containers should be tightly closed when not in use. Should be kept away from moisture.

STORAGE CONDITIONS:

It should be stored in its original unopened package, in a dry, humid-free and cool place (temperature between +5 C and +25 C)

It should not be left under direct sunlight.

.

# SAFETY:

Considering it is a cement based, do not breathe the dust, do not touch the skin and eyes. Use a mask. Use protective gloves, goggles and clothing. In case of eye contact, consult a doctor immediately. Keep out of the reach of children. In case of skin contact, wash with plenty of soap and water. Do not swallow. For detailed information and advice, please refer to the Safety Data Sheet.

# DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from

# misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product.