PROCONTACT

PR 865

# Gross Concrete Primer

PRODUCT DESCRIPTIONS:

It is a water based, acrylic emulsion based, abrasion resistant gross concrete surface primer containing special aggregate.

FEATURES:

It increases the adhesion strength, surface adherence by creating a rough surface for gypsum board bonding on smooth gross concrete floors.

Ready to use.

Environment friendly.

PRODUCT INFORMATION:

Chemical Structure 		Acrylic based / Water based

Aggregate Building 		Basalt

View / Color 			Liquid / Yellow

# PERFORMANCE:

(23°C, %50 Relative Humidity)

Ph			7-10

Density		1,40 ±0,2 g / cm3

Dry film tickness	E3	TS EN 1062-1

Grain Size	S4	TS 2620 EN ISO 1524

These values are obtained as a result of laboratory tests and are valid for the performance of finished applications at the end of full drying time. Since the temperature and humidity values in the construction site and the application surface vary, given values might be diversing.

# APPLICATION AREAS:

It is used on gross concrete which is used on surfaces used such as walls, columns, ceilings.

PROCONTACT

PR 86

# Gross Concrete Primer

# APPLICATION INSTRUCTIONS:

The surface should be cured, dry and sound. Remove oil, grease, dirt, paint and salt vapors that would prevent adhesion. Ready to use. To prepare the product to be ready, 15 kg PROCONTACT PR is mixed with low speed mixer and then applied by brush or roller. It is recommended that the mixture be made with a low speed mixer of less than 500 rpm. Due to the aggregate content, the material in the container should be mixed at intervals during application. Application should not be done before drying. The temperature of the application surface should be 5 °C-30 ° C and the surface should not be rain. After drying, application should be started at least 24 hours later. Application should be between +5 C and +30 C. Do not apply in hot, rainy and windy weather. Do not apply on surfaces with frost hazard. The product must be protected from rain, water, frost and adverse external influences until curing (28 days).

Application Equipment:

Hand Mixer

Brush

Roll

# LIMITATIONS:

To achieve optimum quality, please follow the instructions for use. Application should be between +5 C and +30 C. Do not apply in hot, rainy and windy weather. Do not apply on surfaces with frost hazard. The product must be protected from rain, water, frost and adverse external influences until curing (28 days).

CONSUMPTION:

It depends on the absorbency of the surface.

# PACKING:

15 kg plastic drum

# SHELF LIFE:

It is 1 year from the production date in the original package in dry and humid-free (+5 C to +25 C temperature) environments. The lid of the containers should be tightly closed when not in use. Keep away from moisture.

STORAGE CONDITIONS:

It should be stored in its original unopened package in a cool, dry and humid-free (+5 C to +25 C temperature) environment. Should not be left in direct sunlight.

# SAFETY:

Avoid contact with skin and eyes. Wear protective gloves, glasses, mask and clothing. In case of eye contact, consult a doctor immediately. Keep out of the reach of children. Avoid skin contact. Do not swallow. Keep away from sources of ignition. For further information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product.