PROAQUA

301

Acrylic Resin Based Elastomeric Uv Resistant Waterproofing Product

# PRODUCT DESCRIPTION:

Elastomeric resin based, one-component, uv resistant, smear-based, ready-to-use, super-elastic waterproofing material.

FEATURES::

Due to its elastic structure, it is resistant to temperature differences.

Easy to apply.

Provides seamless appearance.

It has strong penetration.

It has crack bridging capability.

Prevents overheating in summer with reflective feature.

It is resistant to the negative effects of sunlight.

PRODUCT INFORMATION::

Chemical Structure 		Acrylic based / Water based

Appearance / Color 		Liquid / White

# PERFORMANCE:

(23°C, %50 Relative Humidity)

Ph					7-10

Density				1,40 ±0,2 g / cm3

Maximum Pressure 28 days		≥ 4 N

Maximum Streching 28 days		≥1 N/mm2

Adherance (concrete) 28 days	≥1N/mm2

Elongation at break 28 days		≥ %1000

These values are obtained as a result of laboratory tests and are valid for the performance of finished applications at the end of full drying time. Since the temperature and humidity values in the construction site and the application surface vary, given values might be diversing.

# APPLICATION AREAS:

It is used on slopes, roofs and terraces with concrete, plaster, screed, cement plate that uv resistance is demanded.

# APPLICATION INSTRUCTIONS:

Surface should be cured, dry and firm. Remove oil, grease, dirt, paint and salt vapors which prevent adhesion. Surface should be repaired with PROREPAIR THIN or PROREPAIR and in areas where there is sea water, sewage that causes high-sulphate exposition, to be done with the PROREPAIR PLUS at least 24 h before application.The surface of application should be flat and bowless.

It is diluted with 1/1 clean water for primer coat.

Applied without diluting to other 2 layers

PROAQUA

301

Acrylic Resin Based Elastomeric Uv Resistant Waterproofing Product

Application Equipment:

Hand Mixer

Roller brush

Do not apply in rainy, humid weather. Make sure the surface is dry and begin application. PROAQUA is diluted to 1/1 ratio for the primer coat. Otherwise, swelling and adherence weakness will occur. Surface primed in one coat. It is recommended to apply PROBAND splay tape for waterproofing at corner joints. First of all, the application should be done without thinning with a thin brush. After the 24 hours after the priming process, it is applied to the 1st floor horizontal / 2nd floor vertical without diluting with brush or roller. If necessary, the 3rd floor can be applied. The total thickness should be 1-2 mm. Wait 24 hours between coats.

# LIMITATIONS:

In order to obtain optimum quality, please follow the instructions of the application. It should not be applied in very windy, rainy weather which is exposed to sunlight at very high temperature. Do not apply on surfaces with frost hazard. Application area should not be exposed to overload traffic. Application should be between +5 C and +30 C. Do not apply at temperatures below 5 ° C. The product must be protected from rain, water, frost and adverse external influences until curing (28 days).

# CONSUMPTION:

1-1,5 kg/m2 ( for 1 mm thickness)

# PACKING:

1 kg plastic bucket

5 kg plastic bucket

20 kg plastic bucket.

# SHELF LIFE:

In its original package with closed lid, Its 1 year from the date of production in dry and humid-free, no direct sunlight recieving spaces in between ,+5 ̊ - 25   ̊C under the %50 relative humidty. When not in use, cover packaging tightly. Keep away from moisture. Protect from high temperatures and frost.

STORAGE CONDITIONS:

In its original package, it should be stored in a cool, dry (+5 C to +25 C temperature) environment. It should not be left under direct sunlight.

SAFETY:

Do not breathe, wear a mask. Avoid contact with skin and eyes. Wear protective gloves, glasses and clothing. In case of eye contact, consult a doctor immediately. Keep out of the reach of children. In case of contact with skin, wash with plenty of water and soap. Do not swallow. For further information and advice, please refer to the Safety Data Sheet.

DEKOSTAR San. Ve Tic. Ltd. Sti. İs not responsible of application mistakes resulted from misuse or usage without following the instructions and suggestions of DEKOSTAR reserves the right to change its products. Users should consider the lastest edition of the Techical Data Sheet of the product.